# The Mathematical and Phenomenological Framework of Viscoelastic Phase Separation: A Scattering Perspective

## 1. Introduction: The Emergence of Dynamic Asymmetry in Soft Matter

The physics of phase separation in condensed matter is a subject of profound complexity and elegance, governing phenomena ranging from the demixing of metal alloys to the compartmentalization of biological cells. For decades, the theoretical landscape was dominated by two canonical universality classes defined by Hohenberg and Halperin: Model B and Model H. Model B describes phase separation in solid binary mixtures where transport is purely diffusive, governed by the conservation of the order parameter (composition). Model H extends this to fluid mixtures, coupling the conserved order parameter to the transverse momentum density, thereby incorporating hydrodynamic flow. These models rely on a fundamental assumption: dynamic symmetry. They assume that the components of the mixture—whether atoms in an alloy or small molecules in a fluid—possess comparable atomic mobilities and relaxation timescales. Under these conditions, the coarsening of domains proceeds via self-similar growth laws (e.g., the Lifshitz-Slyozov  law or the Siggia  law), and the structure factor  exhibits dynamic scaling, collapsing onto a single universal curve when normalized by the characteristic length scale.

However, the vast majority of "soft matter" systems—polymer blends, colloidal suspensions, protein solutions, and emulsions—are characterized by a profound dynamic asymmetry. In these mixtures, one component (e.g., a long polymer chain or a colloidal particle) moves or relaxes orders of magnitude slower than the other (e.g., a solvent or a smaller molecule). This disparity introduces a new timescale competition: the relaxation time of the slow component () versus the time scale of the phase separation itself. When the deformation rate of the phase-separating domains exceeds the relaxation rate of the slow component, the assumption of local equilibrium breaks down. The slow component cannot rearrange diffusively to accommodate the thermodynamic driving force; instead, it supports mechanical stress.

This regime, where the rheological properties of the components fundamentally alter the kinetics and morphology of demixing, is known as Viscoelastic Phase Separation (VPS).1 Hajime Tanaka and collaborators have rigorously demonstrated that VPS represents a distinct universality class, characterized by unique scattering signatures such as "volume shrinking," "frozen periods," and the formation of transient gels.1

This report provides an exhaustive mathematical and phenomenological framework for VPS, tailored specifically for the interpretation of scattering data (SAXS, SANS, LS). We will derive the governing equations of the two-fluid model, define the critical viscoelastic length scale , and analyze the anomalous evolution of the structure factor  that distinguishes VPS from classical arrested spinodal decomposition.

## 2. Theoretical Foundations: The Two-Fluid Model and Stress Coupling

To understand the scattering signal arising from VPS, we must first establish the equations of motion that generate the density fluctuations. The appropriate theoretical vessel for this analysis is the Two-Fluid Model, originally formulated by Doi and Onuki and significantly extended by Tanaka to include bulk viscoelasticity and dynamic asymmetry parameters.4

### 2.1. The Conserved Order Parameter and Continuity

Consider a binary mixture composed of a polymer (component ) and a solvent (component ). We define the local volume fraction of the polymer as . Assuming the system is incompressible, the solvent volume fraction is . The coarse-grained free energy functional  is typically given by the Ginzburg-Landau (or Flory-Huggins-de Gennes) form:

where  is the local free energy density (e.g., the double-well potential for an unstable quench) and  is the coefficient of the gradient energy penalty, related to the interfacial tension.

The conservation of mass for the polymer component is expressed by the continuity equation:

where  is the macroscopic velocity field of the polymer component.1

In classical Model H (simple fluids), the polymer and solvent move with a single barycentric velocity , and the relative motion is purely diffusive. In the Two-Fluid Model, however, we explicitly treat the velocities of the polymer () and the solvent () as distinct fields. The volume-averaged velocity  is defined as:

Under the incompressibility approximation (), the dynamics are controlled by the relative motion of the two phases.

### 2.2. The Force Balance Equation and Dynamic Asymmetry

The defining mathematical feature of VPS is the force balance equation. In the overdamped limit (where inertial terms are negligible compared to viscous and thermodynamic forces), the total force acting on each component must balance the inter-component friction.

For the polymer component, the force balance is:

For the solvent component:

Here:

- is the thermodynamic driving force (gradient of the chemical potential).

- is the viscoelastic stress tensor supported by the polymer network.1 This term is absent in Model B and usually neglected in Model H.

- is the viscous stress of the solvent (Newtonian).

- is the pressure determined by the incompressibility condition.

- is the friction coefficient per unit volume between the polymer and solvent.

The term  represents the momentum transfer between the phases. In a dynamically asymmetric system, the stress  is orders of magnitude larger than . The polymer network acts as a transient elastic body.

By manipulating these equations, Tanaka derived a generalized convection-diffusion equation for the composition :

Insight: This equation reveals the dual nature of transport in VPS. The first term is the standard Cahn-Hilliard diffusion (driven by thermodynamic potential). The second term is the viscoelastic transport, driven by the divergence of the stress tensor.

- In a typical demixing process, the chemical potential gradient  tries to separate the phases.

- However, phase separation requires the polymer chains to stretch or compress. This generates a viscoelastic stress .

- If the relaxation of  is slow, the stress gradient opposes the chemical potential gradient, effectively suppressing the growth of concentration fluctuations. This is the mathematical origin of the "viscoelastic suppression" of phase separation.8

### 2.3. Constitutive Equations: The Upper Convective Maxwell Model

To close the system, we need a constitutive equation describing how the polymer stress  evolves in time. The most common choice in VPS literature is the Upper Convective Maxwell (UCM) model or the Oldroyd-B model, which properly accounts for frame invariance under large deformations.5

The stress tensor  evolves according to:

This equation contains critical physical parameters:

- Relaxation Time : In VPS, this is not a constant. It depends strongly on the local polymer concentration. In the polymer-rich phase,  can become extremely large (approaching the glass transition or gelation point), while in the solvent-rich phase, it is small. This heterogeneity is key to the formation of "frozen" domains.1

- Plateau Modulus : This represents the elastic energy density of the entangled network. Scaling theory typically predicts  (where  for entangled solutions).

The terms on the left side (the upper convective derivative) describe how the stress tensor is transported and deformed by the polymer velocity field . The "stretching" of the fluid elements by  generates the elastic stress that feeds back into the force balance equation.

### 2.4. The Bulk Stress and Volume Shrinking

A crucial innovation in Tanaka's formulation of VPS is the decomposition of the stress tensor into shear () and bulk () components.6

While classical fluid mechanics often neglects bulk viscosity, it is dominant in VPS. When a polymer network separates from a solvent, it must contract (densify). This isotropic contraction is resisted by the bulk modulus of the network.

- The bulk stress  arises from the volume change of the polymer network relative to the solvent.

- Mathematically, .

- This bulk stress is responsible for the volume shrinking phenomenon observed in scattering. The polymer-rich phase acts like a sponge that is being squeezed. The rate at which it can shrink is limited by the solvent permeation out of the network, a process governed by the balance of the bulk elastic stress and the friction .10

### 2.5. Thermodynamic Consistency and Mathematical Refinements

It is important to note a mathematical subtlety raised in the literature. Early formulations of the VPS model by Tanaka were criticized for lacking full thermodynamic consistency, particularly regarding the Second Law of Thermodynamics. Authors like Zhou, Zhang, and E re-derived the model using an energetic variational approach to ensure dissipation inequalities were strictly satisfied.15 The consistent model introduces an additional pressure term connected to the velocity difference squared, . However, for the purpose of analyzing linear scattering regimes and dominant phenomenological features, Tanaka's original formulation remains the standard "working model" in experimental analysis due to its direct connection to rheological parameters.

## 3. Mathematical Formalism of Dynamic Asymmetry

The term "dynamic asymmetry" is not merely a qualitative descriptor; it introduces a specific set of dimensionless parameters and characteristic length scales that define the scattering behavior.

### 3.1. The Dynamic Asymmetry Parameter ()

Tanaka defines a dimensionless parameter, , to quantify the asymmetry in stress division between the components. In the two-fluid force balance, the stress is not shared equally.

Let  be the fraction of stress supported by component 1 (polymer) and  by component 2 (solvent).

In a simple binary fluid (Model H), the stress is viscous and proportional to the volume fractions (roughly), so  is small or trivial.

In a VPS system (e.g., polymer solution), the polymer network supports all the viscoelastic stress.

- (Polymer supports stress)

- (Solvent supports negligible stress)

- Therefore, .

This parameter  appears directly in the linearized equations of motion. Specifically, the divergence of the relative velocity is coupled to the concentration change via :

This implies that any temporal fluctuation in concentration () inevitably generates a relative velocity field, which in turn generates viscoelastic stress if .1

### 3.2. The Viscoelastic Length Scale ()

The most consequential prediction of the VPS theory for scattering is the existence of a dynamic length scale, , known as the viscoelastic length.8

Derivation logic:

- Consider the competition between the stress relaxation time  (rheology) and the diffusion time  (thermodynamics).

- The cooperative diffusion coefficient is , where  is the osmotic modulus.

- The diffusion time scale for a fluctuation of wavenumber  is .

- The viscoelastic crossover occurs when .

Equating the time scales gives the characteristic length :

Using the scaling relations  (viscosity/modulus), we can express  as:

Physical Interpretation in Scattering ():

The viscoelastic length acts as a screening length for thermodynamic growth.

- Regime 1:  (Large scales). The fluctuations are large and slow. The stress has plenty of time to relax (). The system behaves like a simple fluid (Model H/B). Scattering intensity grows typically.

- Regime 2:  (Small scales). The fluctuations are small and fast. The stress cannot relax on the timescale of diffusion (). The polymer network appears as an elastic solid. The "effective" diffusion coefficient is suppressed.

Experimental measurements on semi-dilute polymer solutions have confirmed that  is typically much larger than the static correlation length (radius of gyration, ). For example, in Polystyrene/Diethyl Malonate systems,  was found to be .8 This confirms that VPS is a mesoscopic effect arising from collective network dynamics, not single-chain elasticity.

### 3.3. The Linear Growth Rate

In the early stages of Spinodal Decomposition (SD), the structure factor grows exponentially: .

Standard Cahn-Hilliard theory predicts:

where  is mobility.

In the VPS framework, the growth rate is modified by the stress storage. The linearized analysis of the Tanaka-Doi-Onuki equations yields a modified amplification factor:

where the effective kinetic coefficient  is -dependent:

Insight: This equation mathematically demonstrates the suppression of short-wavelength fluctuations.

- As  increases (shorter length scales),  decreases.

- Unlike Cahn-Hilliard, where the fastest growing mode  is determined solely by thermodynamics (), in VPS the viscoelastic screening shifts  to smaller values (larger domains) and dampens the overall growth rate. This explains why VPS initially looks "slower" or more arrested than simple fluid demixing.3

## 4. Phenomenology of the Structure Factor in VPS

The mathematical framework described above manifests in distinct features of the scattering structure factor . When analyzing SAXS/SANS/LS data from a VPS system, one observes behaviors that violate the standard scaling laws of Model H.

### 4.1. The "Nonconventional" Evolution of

Classical phase separation is characterized by dynamic scaling:

where  is the peak position. This implies that the domain morphology remains statistically self-similar as it coarsens.

In VPS, this self-similarity breaks down fundamentally due to the volume shrinking of the viscoelastic phase. The evolution of  typically proceeds in three stages 1:

Stage 1: The Frozen Period (Early Stage)

- Observation: The peak position  appears at a finite wavenumber but remains constant () for a significant duration. The intensity  grows exponentially.

- Physics: This is the formation of the transient gel. The polymer-rich phase forms a percolated network. The stress relaxation time is long, effectively "freezing" the domain size at a scale determined by . The network resists the interfacial tension forces that usually drive coarsening.

- Mathematical Condition: The coarsening velocity  is counteracted by the elastic restoring force . The domains are locked in a "force balance" state rather than a hydrodynamic growth state.

Stage 2: Volume Shrinking (Intermediate Stage)

- Observation: This is the hallmark of VPS. The peak position  may remain constant or shift slowly, but the total invariant behaves anomalously. The polymer-rich domains (the network) contract, expelling solvent.

- Violation of Lever Rule: Locally, the volume fraction of the polymer phase increases () while its total volume decreases. This violates the assumption of constant volume fractions used in standard scaling theories.

- Scaling Law: Instead of the classic  (Lifshitz-Slyozov) or  (Siggia), VPS often exhibits anomalous exponents.

  - Tanaka reports transient regimes of  or even arrested growth () depending on the depth of the quench and the viscoelastic relaxation time.10

  - Experimental data on PS/PVME blends show that  is pinned while the intensity increases, reflecting the densification of the network strands rather than the growth of the mesh size.19

Stage 3: Phase Inversion and Late Stage

- Observation: Eventually, the solvent expulsion renders the polymer-rich phase so dense that it occupies a minority of the volume. The connectivity of the network breaks (mechanical fracture or disentanglement), and the system "inverts." The polymer-rich phase transforms from a continuous matrix into discontinuous droplets.

- Scattering Signature: This transition is often sudden. The structure factor may develop a secondary peak or shoulder, corresponding to the new droplet size, while the original network peak vanishes. Following inversion, normal Model H coarsening ( or ) may resume if the droplets are fluid enough.13

### 4.2. Comparison with Arrested Spinodal Decomposition

It is vital to distinguish VPS from Arrested Spinodal Decomposition (ASD), often observed in colloidal gels. While both show "arrested" scattering peaks, the mechanics differ.21

| Feature | Viscoelastic Phase Separation (VPS) | Arrested Spinodal Decomposition (ASD) |
| --- | --- | --- |
| Mechanism | Dynamic asymmetry Stress supports network. | Glass transition/Jamming of particle-rich phase. |
| Kinetics | Transient arrest followed by volume shrinking and often phase inversion. | Permanent arrest (on exp. timescales). No volume shrinking. |
| Structure Factor | Peak intensity grows while is fixed (densification). | Peak intensity and both freeze (structure locked). |
| Material | Polymer solutions, protein condensates (liquid-like to solid-like transition). | Deep quench colloids, attractive glasses (solid-like). |

Mathematically, ASD is a thermodynamic arrest line crossing the spinodal. VPS is a kinetic trajectory where the system fights its way to equilibrium through mechanical stress. The observation of volume shrinking (densification of the scattering objects) is the definitive proof of VPS over ASD.

### 4.3. The Furukawa Scaling Function in VPS

The universality of phase separation is often tested by plotting the scaled structure factor  against the reduced wavenumber .

For Model B/H, the data collapse onto the Furukawa Function:

where  depends on dimensionality (usually  for 3D, yielding Porod's tail).

In VPS, deviations from Furukawa scaling are prevalent.23

- Broadening of the Peak: The distribution of domain sizes is wider in VPS due to the spatial heterogeneity of the viscoelastic relaxation. Parts of the network relax and coarsen, while others remain frozen. This broadens the main peak of .

- Porod Tail Anomalies: While the high- limit usually follows Porod's law () indicating sharp interfaces, the "shoulder" region often exhibits excess scattering. This arises from the internal structure of the polymer network itself (the "gel" structure inside the domains), which acts as a mass fractal.

## 5. Fractal Analysis of the Transient Network

The transient gel formed during VPS is a disordered, connected structure. Scattering at intermediate wavenumbers (between the domain size  and the monomer size ) probes the internal geometry of this network. This requires a fractal analysis framework.

### 5.1. Mass Fractals vs. Surface Fractals

The scattering intensity  generally follows a power law . The exponent  reveals the topology:

- Mass Fractal ():
If the exponent  is between 1 and 3, the object is a mass fractal. This means the mass  scales with radius  as .

  - In VPS, the "sponge-like" network structure often exhibits mass fractal scaling (e.g., ) in the intermediate  range.25 This reflects the random branching and crosslinking of the transient polymer strands.

- Surface Fractal ():
If the exponent  is between 3 and 4, the object is a surface fractal.

  - corresponds to a smooth surface (, Porod's Law).

  - corresponds to a maximally rough surface ().

  - In the late stages of VPS, as the domains densify and interfaces sharpen, the scattering transitions from mass fractal behavior (network) to surface scattering (compact domains with Porod tails).27

### 5.2. The Beaucage Unified Model

To mathematically fit the scattering data of a VPS system across multiple length scales (from the large domains down to the network mesh), the Beaucage Unified Exponential/Power-Law model is the industry standard.28 It seamlessly stitches together Guinier (radius of gyration) and Power-Law (fractal) regimes.

For a VPS transient gel, a two-level model is typically required:

- Level 1 (Large Scale - Domains):

  - : Radius of the phase-separated domains ().

  - : Usually 4 (Porod) or close to 4, representing the sharp interface between the polymer-rich phase and the solvent-rich phase.

- Level 2 (Small Scale - Network):

  - : The correlation length or mesh size  of the internal network.

  - : The mass fractal dimension  (typically ~2.2 for swollen gels).

Using the Beaucage model allows the researcher to deconvolve the growth of the domains () from the densification of the network ( constant,  or ). This provides quantitative proof of the hierarchical structure inherent to VPS.

### 5.3. The Berry-Russel Model (Rod-like Systems)

While the Beaucage model is general, specific types of VPS involve rigid rods (e.g., liquid crystal polymers, cellulose whiskers). Here, dynamic asymmetry arises from rotational diffusion constraints. The Berry-Russel model is often cited for such systems.31

This model incorporates the orientationally pre-averaged interaction between rods. It is useful when the scattering does not show a distinct correlation peak (due to disorder) but exhibits a suppression of intensity at low  due to the repulsive interactions or excluded volume that drives the gelation. In VPS of rods, this model helps distinguish between simple aggregation and thermodynamically driven demixing arrested by jamming.

## 6. Complex Systems: Polyelectrolytes and Charge Effects

Recent research has expanded the VPS framework to polyelectrolyte (PE) solutions, which are critical for understanding biological condensates (e.g., membraneless organelles, RNA/protein droplets).2

In neutral polymers, dynamic asymmetry is driven by chain entanglement (). In PEs, electrostatic interactions introduce a competing length scale (Debye length ) and interaction parameter (Bjerrum length ).

### 6.1. Charge Symmetry vs. Asymmetry

Experimental studies 2 distinguish two cases based on the chain lengths of the polycation () and polyanion ():

- Charge Symmetry ():

  - The viscoelastic effects are minimized because the chains can form neutral pairs that diffuse relatively fast.

  - Scattering  often restores self-similarity.

  - Scaling laws like  have been observed, distinct from the arrested VPS behavior.

- Charge Asymmetry ():

  - One chain is much longer than the other. The long chain forms a scaffold (network) while the short chain acts like a crosslinker or solvent.

  - This restores dynamic asymmetry. The system exhibits classic VPS signatures: volume shrinking, deviation from power-law coarsening, and "frozen" peaks in .

  - Insight: The electrostatic attraction acts as an "effective" deep quench, tightening the network and enhancing the bulk modulus , which accelerates volume shrinking compared to neutral VPS.

### 6.2. The Electrostatic-Viscoelastic Analogy

Mathematically, the PE-VPS system can be mapped onto the neutral VPS model by modifying the local free energy  to include the Voorn-Overbeek (or RPA) electrostatic term, and modifying the friction  to account for ion pairing.

The key finding is that electrostatics controls the quench depth, while chain asymmetry controls the viscoelastic braking. The scattering peak in PE-VPS arises from the micro-phase separation of the coacervate droplets, and its arrest is governed by the same  logic as in neutral polymers.

## 7. Experimental Case Studies and Applications

### 7.1. Polystyrene (PS) / Poly(vinyl methyl ether) (PVME)

This is the canonical system studied by Tanaka.

- Dynamic Asymmetry: PS has a high  (slow), PVME has a low  (fast). By adjusting temperature relative to the  of the blend, one can tune .

- Scattering: SAXS data clearly show the "frozen period" where  is constant for minutes, followed by a sudden drop (coarsening) during phase inversion.

- Volume Shrinking: Time-resolved measurement of the invariant shows a decrease in the scattering volume of the PS-rich phase, confirming it is densifying.19

### 7.2. Biological Condensates (RNA/Protein)

VPS is now the leading physical model for the formation of stress granules and nucleoli in cells.

- Observation: These droplets often are not simple liquids; they are viscoelastic. They show incomplete fusion and non-spherical shapes.

- Scattering Relevance: VPS explains why these droplets don't coarsen indefinitely (Ostwald ripening). The viscoelastic stress stabilizes a specific droplet size distribution (), crucial for cellular function (compartmentalization without total phase separation).2

## 8. Conclusion

The mathematical framework of Viscoelastic Phase Separation transforms our understanding of demixing in complex fluids. It replaces the diffusive paradigm of Model B and the hydrodynamic paradigm of Model H with a stress-diffusion coupling model.

For the researcher employing scattering techniques, VPS is identifiable not just by "slow dynamics," but by a specific set of mathematical signatures:

- The Viscoelastic Length : A crossover scale separating Newtonian and Elastic dynamics, defined by .

- Kinetic Anomalies: The arrest of  (frozen period) and the non-conservation of the phase volumes (volume shrinking), violating standard dynamical scaling laws ().

- Fractal Geometry: The emergence of mass fractal scattering () from the transient gel network, quantifiable via the Beaucage model.

- Dependence on Dynamic Asymmetry: The severity of these effects scales with the asymmetry parameter , linking the microscopic molecular weights and s to the macroscopic pattern formation.

By integrating the Two-Fluid Model's stress tensor with the fractal analysis of the structure factor, one obtains a complete toolkit for decoding the complex scattering patterns of dynamically asymmetric soft matter.

## 9. Summary Table of Key VPS Parameters

| Parameter | Symbol | Definition/Approximation | Physical Significance in Scattering |
| --- | --- | --- | --- |
| Structure Factor |  |  | Primary observable; measures domain correlations. |
| Viscoelastic Length |  |  | Crossover length; modes are suppressed. |
| Dynamic Asymmetry |  |  | Coupling strength between and stress. |
| Relaxation Time |  |  | Time scale of stress decay; strongly -dependent. |
| Growth Rate |  |  | Linear stability eigenvalue; suppressed by . |
| Fractal Dimension |  | Slope of vs | Topology of the transient gel (). |
| Unified Parameter |  | Beaucage Exponent | Distinguishes Mass Fractal () from Surface (). |
| Porod Invariant |  |  | Total scattering power; anomalous evolution in VPS. |

#### Works cited

- (PDF) Viscoelastic phase separation - ResearchGate, accessed on December 17, 2025, https://www.researchgate.net/publication/230930882_Viscoelastic_phase_separation

- Network-forming phase separation of oppositely charged polyelectrolytes forming coacervates in a solvent - PMC - PubMed Central, accessed on December 17, 2025, https://pmc.ncbi.nlm.nih.gov/articles/PMC11828884/

- Critical dynamics and phase-separation kinetics in dynamically asymmetric binary fluids, accessed on December 17, 2025, https://pubs.aip.org/aip/jcp/article-pdf/100/7/5323/19070941/5323_1_online.pdf

- New dynamic universality class for polym - Sci-Hub, accessed on December 17, 2025, https://2024.sci-hub.se/3373/29147d8a623c9b889ec261808c328c19/tanaka1994.pdf

- arXiv:cond-mat/0310228v1 [cond-mat.soft] 9 Oct 2003, accessed on December 17, 2025, https://arxiv.org/pdf/cond-mat/0310228

- Network formation in viscoelastic phase separation - SciSpace, accessed on December 17, 2025, https://scispace.com/pdf/network-formation-in-viscoelastic-phase-separation-k8jzfzsmv8.pdf

- Viscoelastic Phase Separation of Softmaterial | Request PDF - ResearchGate, accessed on December 17, 2025, https://www.researchgate.net/publication/275567424_Viscoelastic_Phase_Separation_of_Softmaterial

- Experimental studies of stress–diffusion coupling in semi-dilute polymer solutions. I. 'Viscoelastic length' and viscoelastic effects on early stage spinodal decomposition | Request PDF - ResearchGate, accessed on December 17, 2025, https://www.researchgate.net/publication/223538669_Experimental_studies_of_stress-diffusion_coupling_in_semi-dilute_polymer_solutions_I_'Viscoelastic_length'_and_viscoelastic_effects_on_early_stage_spinodal_decomposition?_share=1

- Shin Saito's research works | Kyoto University and other places - ResearchGate, accessed on December 17, 2025, https://www.researchgate.net/scientific-contributions/Shin-Saito-9657043

- Viscoelastic phase separation in soft matter and foods - RSC Publishing, accessed on December 17, 2025, https://pubs.rsc.org/en/content/articlehtml/2012/fd/c2fd20028g

- Energy-stable numerical schemes for multiscale simulations of polymer-solvent mixtures - Numerik, accessed on December 17, 2025, https://www.numerik.mathematik.uni-mainz.de/files/2017/07/Journals-66.pdf

- Modelling and numerical simulation of phase separation in polymer modified bitumen by phase-field method - DiVA portal, accessed on December 17, 2025, https://www.diva-portal.org/smash/get/diva2:939564/FULLTEXT01.pdf

- Phase Inversion during Viscoelastic Phase Separation: Roles of Bulk and Shear Relaxation Moduli - ResearchGate, accessed on December 17, 2025, https://www.researchgate.net/publication/255658049_Phase_Inversion_during_Viscoelastic_Phase_Separation_Roles_of_Bulk_and_Shear_Relaxation_Moduli

- (PDF) Volume-shrinking kinetics of transient gels as a consequence of dynamic interplay between phase separation and mechanical relaxation - ResearchGate, accessed on December 17, 2025, https://www.researchgate.net/publication/329926194_Volume-shrinking_kinetics_of_transient_gels_as_a_consequence_of_dynamic_interplay_between_phase_separation_and_mechanical_relaxation

- Existence and weak-strong uniqueness for global weak solutions for the viscoelastic phase separation model in three space dimensions, accessed on December 17, 2025, https://www.aimsciences.org/article/doi/10.3934/dcds.2023004

- Thermosensitive Diblock Copolymer of Poly(N-isopropylacrylamide) and Poly(ethylene glycol) in Water: Polymer Preparation and Solution Behavior | Request PDF - ResearchGate, accessed on December 17, 2025, https://www.researchgate.net/publication/231696505_Thermosensitive_Diblock_Copolymer_of_PolyN-isopropylacrylamide_and_Polyethylene_glycol_in_Water_Polymer_Preparation_and_Solution_Behavior

- Morphology and Dynamics of Phase‐Separating Fluids with Viscosity Asymmetry | Request PDF - ResearchGate, accessed on December 17, 2025, https://www.researchgate.net/publication/229749432_Morphology_and_Dynamics_of_Phase-Separating_Fluids_with_Viscosity_Asymmetry

- Structure formation and coarsening kinetics of phase-separated spin-coated ethylcellulose/hydroxypropylcellulose films. - R Discovery, accessed on December 17, 2025, https://discovery.researcher.life/article/structure-formation-and-coarsening-kinetics-of-phase-separated-spin-coated-ethylcellulose-hydroxypropylcellulose-films/2f5dad88d11b3c15ade816e559350ccb

- Analysis of a viscoelastic phase separation model - ResearchGate, accessed on December 17, 2025, https://www.researchgate.net/publication/349736724_Analysis_of_a_viscoelastic_phase_separation_model

- Phase Separation Kinetics of a Polymer Blend Modified by Random and Block Copolymer Additives | Request PDF - ResearchGate, accessed on December 17, 2025, https://www.researchgate.net/publication/231711927_Phase_Separation_Kinetics_of_a_Polymer_Blend_Modified_by_Random_and_Block_Copolymer_Additives

- Gelation dynamics upon pressure-induced liquid-liquid phase separation in a water-lysozyme solution - PUBDB, accessed on December 17, 2025, https://bib-pubdb1.desy.de/record/486316/files/2107.05026v1.pdf

- Real space analysis of colloidal gels: triumphs, challenges and future directions - CentAUR, accessed on December 17, 2025, https://centaur.reading.ac.uk/101361/1/Royall_2021_J._Phys.__Condens._Matter_33_453002.pdf

- (PDF) Ageing and collapse in gels with long-range attractions - ResearchGate, accessed on December 17, 2025, https://www.researchgate.net/publication/228924099_Ageing_and_collapse_in_gels_with_long-range_attractions

- Confinement-induced screening of hydrodynamic interactions and spinodal decomposition: Multiscale simulations of colloid-polymer mixtures | Request PDF - ResearchGate, accessed on December 17, 2025, https://www.researchgate.net/publication/258276078_Confinement-induced_screening_of_hydrodynamic_interactions_and_spinodal_decomposition_Multiscale_simulations_of_colloid-polymer_mixtures

- Small angle neutron scattering - EPJ Web of Conferences, accessed on December 17, 2025, https://www.epj-conferences.org/articles/epjconf/pdf/2015/23/epjconf-jdn_01004.pdf

- Small-Angle Scattering from Fractals: Differentiating between Various Types of Structures, accessed on December 17, 2025, https://www.mdpi.com/2073-8994/12/1/65

- Small-Angle Scattering from Mass and Surface Fractals - Semantic Scholar, accessed on December 17, 2025, https://pdfs.semanticscholar.org/0676/d3aa970057114a43157a5dd8bc5c3c15d71d.pdf

- Small-Angle Scattering from Polymeric Mass Fractals of Arbitrary Mass-Fractal Dimension - College of Engineering and Applied Science, accessed on December 17, 2025, https://www.eng.uc.edu/~beaucag/PDFPapers/Beaucage1.pdf

- Unified scattering function - Wikipedia, accessed on December 17, 2025, https://en.wikipedia.org/wiki/Unified_scattering_function

- unified_power_Rg — SasView 6.1.1 documentation, accessed on December 17, 2025, https://www.sasview.org/docs/user/models/unified_power_Rg.html

- thermal transport of nanofluids in a minichannel - UH Institutional Repository, accessed on December 17, 2025, https://uh-ir.tdl.org/server/api/core/bitstreams/f3b51e0a-8b89-4286-a4fd-9d033e09f734/content

- Laminar convective heat transfer of alumina-polyalphaolefin nanofluids containing spherical and non-spherical nanoparticles - APPLIED ELECTROMAGNETICS LABORATORY, accessed on December 17, 2025, http://www2.egr.uh.edu/~dli9/2011_etfs_pao-nanofluids.pdf

- Viscoelasticity of suspensions of long, rigid rods | Request PDF - ResearchGate, accessed on December 17, 2025, https://www.researchgate.net/publication/223714978_Viscoelasticity_of_suspensions_of_long_rigid_rods

- The Dynamical Asymmetry in SARS-CoV2 Protease Reveals the Exchange Between Catalytic Activity and Stability in Homodimers - PubMed Central, accessed on December 17, 2025, https://pmc.ncbi.nlm.nih.gov/articles/PMC11990344/